## Slide 1
2014
Washington Asphalt Conference
“Specification Update & Initiatives”
Joe DeVol
Assistant State Materials Engineer
State Materials Laboratory

## Slide 2: Specification Updates
2014 Updates
  4-06 & 9-03.6 - Asphalt Treated Base
    Deleted - unused and incompatible with Superpave specifications
  9-03.8(4) - Blending Sand
    Deleted - considered part of mineral aggregate

## Slide 3: Specification Updates
2014 Updates
  9-03.8(1) - General Requirements
    Added Sand Equivalent requirement to aggregate source approval
    Restricted amount of No. 4 minus material - 5 percent by total weight of aggregate

## Slide 4: Specification Updates
2014 Updates
  5-04.3(3)A - Material Transfer Device/Vehicle
    Amended - Engineer authority to exclude where not feasible

## Slide 5: Specification Updates
2014 Updates
  5-04.3(7)A1 - General Contractor Mix Design Requirements
    AASHTO T 324 - Hamburg Wheel-Track Testing
    ASTM D 6931 - Indirect Tensile Strength (IDT)
    Brand and type of anti-stripping additive, certificate of compatibility
Optional See GSP

## Slide 6: Specification Updates
2014 Updates
  5-04.3(7)A2 - Statistical or Nonstatistical Evaluation Contracting Agency Evaluation
    AASHTO T 324 - Hamburg Wheel-Track Testing
    ASTM D 6931 - Indirect Tensile Strength (IDT)

## Slide 7: Specification Updates
2014 Updates
  9-03.8(2) - HMA Test Requirements
  Hamburg & IDT

## Slide 8: Specification Updates
Mix Criteria | HMA Class |  |  |  |  |  |  | 
 | ⅜ inch |  | ½ inch |  | ¾ inch |  | 1 inch | 
 | Min. | Max. | Min. | Max. | Min. | Max. | Min. | Max.
Hamburg Wheel-Track Testing, WSDOT FOP for AASHTO T 324 Rut Depth (mm) @ 15,000 Passes |  | 10 |  | 10 |  | 10 |  | 10
Hamburg Wheel-Track Testing, WSDOT FOP for AASHTO T 324 Minimum Number of Passes With no Stripping Inflection Point | 15,000 |  | 15,000 |  | 15,000 |  | 15,000 | 
Indirect Tensile (IDT) Strength (psi) of Bituminous Materials WSDOT FOP for ASTM D 6931 |  | 175 |  | 175 |  | 175 |  | 175

## Slide 11: Specification Updates
2014 Updates
  5-04.3(10)B1 - General
    Added use of roadway cores to determine pavement density
    For use when practical & cost effective
    Includes bid item for Contractor coring

## Slide 12: Specification Updates
2014 Updates
  5-04.3(10)B3 -Longitudinal Joint Density
  Deleted – now testing within 0.5’ of joint

## Slide 13: Specification Updates
2014 Updates
  5-04.3(20) - Anti-Stripping Additive
    Added to the liquid asphalt prior to shipment
  5-04.5 - Payment
    Bid price for HMA includes anti-stripping additive

## Slide 14: Specification Updates
2015 Updates
  QPL Mix Design Approval Process
  HMA Mixture & Density Test Sub-lot Sample Size Changes
  High RAP & RAS - GSP to Standard Specification
  5-04.3(13) Surface Smoothness – revisions pending

## Slide 15
2014
Questions?
Washington Asphalt Conference
“Specification Updates & Initiatives”