## Slide 1
Paving Potpourri
2015 Spec Changes and More!
Bob Dyer
Assistant State Construction Engineer
WAPA Joint Training
March 2015
Lynn Peterson
Secretary of Transportation

## Slide 2: Spec Changes – Done Deal
Eliminate Anti-Strip in temp HMA
RAP/RAS
  Current RAP/RAS will be an amendment in April 2015
Density Acceptance by Cores
  Bid item for projects we want Contractor to core

## Slide 3: Spec Changes – Done Deal
Pavement Smoothness
  January 2015 GSP
Mix Design Approval with QPL
  April 2015

## Slide 4: Spec Changes – Done Deal
HMA Mix | 
HMA Project Quantity (tons) | Sublot Size (tons)
<20,000 | 1,000
20,000 to 30,000 | 1,500
>30,000 | 2,000
HMA Density | 
HMA Project Quantity (tons) | Sublot Size (tons)
<20,000 | 100
20,000 to 30,000 | 150
>30,000 | 200
As of January 2015
Mix Sublot size
From 1/800T to 1/1000T
Density Sublot size From 1/80T to 1/100T
  As of April 2015
Test Frequency

## Slide 5: Spec Changes – Coming but not Finalized
Increase in RAP Percent
  Nationally 0-15% OK; 15-25 drop a binder grade; >25 detailed mix design (like what we do now)
HMA On bridge decks
  Should be something (GSP or amendment) by August 2015

## Slide 6: HMA Points of Emphasis
Old Way
Pass/Fail with tolerance on an individual test
Today’s Way:
Statistical Evaluation

## Slide 7: HMA Points of Emphasis
Standard Spec 3-04
  Fine Aggregate Angularity
  Sand Equivalent
  Coarse Aggregate Fracture

## Slide 8
Chart: Hot Mix Asphalt, Asphalt Binder & Crude Oil Indices
| Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014
WSDOT HMA | 100 | 112.691 | 119.2412 | 109.7761 | 104.1346 | 124.089 | 113.6439 | 98.9889 | 129.6457 | 145.2289 | 142.1662 | 115.8044 | 129.0301 | 148.2362 | 153.8776 | 145.3969 | 180.707 | 190.6475 | 204.6769 | 179.1735 | 194.788 | 212.346 | 274.6776 | 180.4466 | 199.1624 | 232.9474 | 335.2311 | 294.9602 | 243.8164 | 211.8033 | 209.6817 | 238.7288 | 215.6296 | 208.6008 | 213.8582 | 195.6533 | 218.4601 | 212.2804 | 237.014 | 218.8365 | 240.7546 | 258.3549 | 302.2719 | 291.5404 | 249.6933 | 242.4327 | 343.5665 | 212 | 251.9815 | 261.053 | 300.9793 | 436.552
EIA CRUDE | 100 | 121.0267 | 130.6794 | 130.1106 | 157.3778 | 133.6305 | 139.3022 | 143.8364 | 162.5115 | 176.8214 | 202.3055 | 222.7175 | 229.296 | 244.6357 | 291.3618 | 276.6523 | 291.7307 | 324.6695 | 324.7002 | 276.5601 | 267.7989 | 299.4466 | 301.8598 | 418.4752 | 451.5985 | 571.5646 | 544.3436 | 268.675 | 197.8789 | 274.0854 | 314.4943 | 350.7224 | 362.6191 | 358.6996 | 350.6916 | 392.3916 | 431.3095 | 471.3956 | 414.3713 | 433.5075 | 474.3774 | 430.8023 | 425.0537 | 405.5948 | 434.9984 | 418.5367 | 488.0563 | 448.8625 | 455.3335 | 476.5447 | 450.876 | 337.3501
WSDOT ASPHALT BINDER | 100.0024 | 103.9366 | 124.4685 | 123.8153 | 132.901 | 135.2467 | 130.6444 | 124.7061 | 124.7061 | 128.5363 | 133.3761 | 134.6825 | 135.2467 | 133.2217 | 134.7419 | 144.0355 | 172.807 | 216.9446 | 276.4614 | 267.3757 | 259.2698 | 248.2696 | 247.6306 | 245.9085 | 254.4906 | 342.2742 | 525.1776 | 422.6062 | 370.9708 | 347.8111 | 342.7195 | 327.9472 | 342.1257 | 361.5442 | 348.747 | 327.8581 | 335.0887 | 379.9532 | 418.1026 | 389.1292 | 403.4989 | 440.628 | 433.7253 | 410.3126 | 399.4311 | 392.4547 | 389.261 | 379.5221 | 371.0896 | 399.8777 | 425.2928 | 419.3841

## Slide 9: Hot Mix Asphalt Unit Bid Price
Chart: $ / TON
| 90 | 91 | 92 | 93 | 94 | 95 | 96 | 97 | 98 | 99 | 00 | 01 | 02 | 03 | 04 | 05 | 06 | 07 | 08 | 09 | 10 | 11 | 12 | 13 | 14
HOT MIX ASPHALT | 32.8165 | 28.6246 | 26.4777 | 27.2255 | 27.832 | 28.2775 | 28.069 | 31.3461 | 31.0981 | 28.5392 | 31.6879 | 32.0056 | 33.508 | 34.7825 | 40.5891 | 42.6371 | 57.1199 | 61.3556 | 66.0822 | 67.4448 | 63.4365 | 66.1684 | 80.1475 | 71.3401 | 78.5112

## Slide 10
Government Regulation and Taxes

## Slide 11
Government Regulation and Taxes

## Slide 12: Bob Dyer
Assistant State Construction Engineer, Roadway
DyerB@wsdot.wa.gov
360.705.6980